Evan Huling

Dr. Joshua Klaassen

Self-Densified Super-Strong Wood

October 7, 2025

INTRODUCTION

In my research I will be attempting to create a super-strong wood by putting natural wood blocks through a self-densification process. The process will be based upon the process described in “Self-densified super-strong wood” by Huang and his colleagues. This involves the delignification of a natural wood block by immersing the block in a boiling solution of 2.5M NaOH and 0.3M Na2SO3, then the cellulose activation by N,N-dimethylacetamide. This research is relevant due to the need to find new materials to lower the world’s reliance on non-renewable resources. While there have been many studies on processes to create a stronger version of wood, many face difficulties like the processes being too costly to perform efficiently or require substances that are very harmful to the environment. An example of one of these hazardous chemicals is N,N-dimethylacetamide, which can contaminate water sources if released into the environment. One of my goals for this research is to firstly replicate the findings of Zhu et al. and then attempt to find a more environmentally friendly process by substituting out N,N-dimethylacetamide for a different solution. I also want to find more uses for the self-densification process, aside from the evident superstrong properties.

BODY

The article “Self-densified super-strong wood” published by Huang and his colleagues describes an experiment that studied the process of inducing self-densification of wood. This study is the main experiment that I am basing my research out of. This process of self-densification starts by immersing wood blocks into a “boiling lignin removal solution of mixed NaOH solution (2.5 mol/L) and Na2SO3 solution (0.3 mol/L) for 10 h,” the wood was then “immersed in boiling deionized water several times to remove residual chemicals” (Huang et al., 2025). Next the wood cellulose is activated by submerging the partially delignified (DLW) into N,N-dimethylacetamide for 1 h at 160℃, followed by the addition of LiCl to induce the swelling reaction of the wood. Residual chemicals were then rinsed out of the swelling wood with deionized (DI) water. Finally, the wood was left out to dry, which allowed it to spontaneously self-densify to create the self-densified super-strong wood (SSW). The SSW had its properties tested compared to natural wood and compressed wood. One test performed recorded the tensile strengths of the different wood types, with the tensile strength of the SSW being “approximately 496.1 MPa, which is 9.0 times higher than that of the original wood (55.3 Mpa)” (Huang et al., 2025). The SSW also exhibited an impressive specific strength with values as high as 396.8Mpa/(g*cm-3), which makes “it a promising new ultra-lightweight engineering material” (Huang et al., 2025). The SSW also possessed a high toughness with “its fracture work exceeding ten times that of natural wood” and an “impact toughness of 75.2 kJ/m2,” which is “six times greater than natural wood” (Huang et al., 2025). The SSW also had a higher compressive strength and a higher flexural strength when compared to natural wood and compressed wood. Many of these improvements in the properties of the wood are due to the nature of the self-densification process. One of the reasons behind this is because the self-densification process allows the wood to maintain an ordered structure, with the wood compounds collapsing in to become more tightly packed. The self-densification process also promotes the formation of many new hydrogen bonds due to the abundant number of hydroxyl groups found in the swelling and dehydration steps of the process. This study also tested the functionality of a nail produced from the SSW, which this test yielded promising results with the SSW nail outperforming steel nails in two categories. With those two categories being that it had a better nail-holding ability and caused less damage to the wood. This provides a source of high-quality nails from a renewable resource.

The article “Delignification and ionic liquid treatment of wood toward multifunctional high-performance structural materials” Khakalo and his colleagues’ study the process of delignifying wood and then treating the delignified wood with an ionic liquid (IL). Their goal was to find a new multifunctional substance. To start the experiment, they delignified the wood with 1 wt% sodium chlorite to create partially delignified wood (DLW). This DLW was then treated with an IL composed of 1-ethyl-3 methylimidazolium acetate under both atmospheric conditions and under a vacuum. This IL treated wood was then “heated in an oven at 95℃ either for 1 or 6 h” (Khakalo et al.). The wood was then kept in purified water and rinsed until the washing water was clear, this removed the residual IL from the samples. The samples were then “dried in a hot press under 5 Mpa at 100 °C overnight” (Khakalo et al.). The wood that was heated for 1 h had a lower density (1250 kg/m3) than that of the wood heated for 6 h (1335 kg/m3). While the wood heated for 1 h had better mechanical properties. This is because the extra heating caused the crystalline structure of the treated wood to undergo a more dramatic change in its crystalline structure. This change in the structure resulted in a new crystalline structure that is held together by weaker bonds. An additional finding of the IL treated wood was the “limited permeability of gas, grease, and water vapor because of the dense and well-packed structure” (Khakalo et al.). The IL treated wood was also found to be partially transparent due to it losing much of its structural matrix. Another part of the study was to create different shapes of the treated wood. This was achieved by having two molds, a female mold to place the wet IL treated wood in, and a male pin guided mold to press the wood into the correct shape. This wood in the mold was pressed at 100℃ until the wood was dried. This yielded promising results.

CONCLUSION

The findings of both Huang and Khakalo provide significant contributions to finding a method to use wood as a replacement for many nonrenewable resources. Huang provided a method to create a super-strong wood that can be used as a replacement for many steel products. This process greatly increased the mechanical properties of the wood and leads to many theoretical uses for self-densified wood. The main example that the study used was of a wooded nail made of self-densified wood, which ended up outperforming steel nails in ability to hold as a nail, and it didn’t cause as much damage to the wooden backboard as steel nails. Khakalo provided a solution to creating a very strong and flexible multifunctional resource out of wood through partial delignification and then ionic liquid treatment. This treatment of wood increased the mechanical properties of wood, while also increasing the flexibility of the wood. The study also found a way to mold the DLW into more useful shapes after its IL treatment. While these articles are very beneficial to the movement of using mainly renewable resources instead of steel-based and petroleum-based resources, there are a few shortcomings. One of which being the fact that some of the solutions required are very harmful to the environment, for example N,N-dimethylacetamide can contaminate entire reservoirs if released into the environment. Another shortcoming is that they didn’t test the flammability of the treated wood, which should be an essential test because of the flammable nature of normal wood and many proposed uses wouldn’t work if the treated wood was very flammable. But with all things considered, these findings will be very important for the advancement of using only renewable resources because the findings of these experiments can be used for many problems. For example, the self-densified wood can be used to replace steel support beams in house construction.

Work Cited

Huang, D., Li, J., Li, S., Cao, Z., Guo, Y., Ding, Y., Zhu, M., & Chen, Y. (2025). Self-densified super-strong wood. Journal of Bioresources and Bioproducts, 10(2), 199-208. Self-densified super-strong wood - ScienceDirect

Khakalo, A., Tanaka, A., Korpela, A., & Orelma, H. (2020). Delignification and ionic liquid treatment of wood toward multifunctional high-performance structural materials. ACS Applied Materials & Interfaces, 12(20), 23532-23542, https://pubs.acs.org/doi/10.1021/acsami.0c02221

Liu, Y., Li, B., Mao, W., Hu, W., Chen, G., Liu, Y., & Fang, Z. (2019). Strong Cellulose-based materials by coupling sodium hydroxide-anthraquinone (NaOH-AQ) pulping with hot pressing from wood. ACS Omega, 4(4), 7861-7865. https://pubs.acs.org/doi/10.1021/acsomega.9b00411